ANTISTAT-340

SEMA HWASUNG Co., Ltd.

Tel : (02)927-7842~4 / Fax : (02)927-7845

Description : special anionic compounds

∙ TYPICAL PROPERTIES

- appearance	:  yellowish paste

- PH	:  7 ± 0.5

- density (25℃) :  app 0.95/㎤

- moisture %	:  4max

- solubility	:  soluble in toluene

∙ APPLICATION

- ANTISTAT-340 has been developed as an internal antistatic agent for many thermo- plastics and photogravure ink.

- ANTISTAT-340 can eliminate electrostatic trouble and dust problem.

- ANTISTAT-340 is specially suitable for UV curing ink.

∙ DOSAGE

- 1 ~ 2% for photogravure ink.