HYCEL-T

SEMA WHASUNG Co., Ltd.

Tel : (02)927-7842~4 / Fax : (02)927-7845

HYCEL-T is a compound of fatty acid glyceryl ester made from edible, It has excellent performance of antishrinking agent for polyethylene foam which is generally recognized as safe for food packing material.

• PHYSICAL DATE

Appearance	white powder

Iodine value	2 max

Free glycerol(%)	1 max

Free fatty acid(%)	1.5 max

Melting point	approx. 70℃

• PACKING

25kg net in paper bag.